Scanning Hall Probe Microscopy: QuantItatIve & Non-InvasIve Magnetıc ImagIng and Magnetometry at 50 nanometer scale

Ahmet Oral

Bilkent University, Department of Physics, 06800 Ankara, TURKEY

Scanning Hall Probe Microscopy (SHPM)[1,2] is a quantitative and non-invasive technique for imaging localized surface magnetic field distribution on sample surfaces with high spatial and magnetic field resolution of  ~50nm & 1G/Hz, over a wide range of temperatures, 30mK-300K. In SHPM, a nano-Hall probe is scanned over the sample surface to measure the perpendicular component of the surface magnetic fields using STM[1] or AFM[3] positioning techniques as shown in Fig.1. SHPM is a quantitative and non-invasive method, compared to MFM with similar spatial resolution. The nano-Hall sensor’s used in the SHPMs do not saturate under high external fields and the technique has been shown to operate up to 9T. SHPMs[4] can be run at fast scanning speeds, ~1 frame/s to obtain time resolved magnetic images. The microscope can also be used as a local scanning magnetometer with extremely high magnetic moment sensitivity and can measure magnetization loops of individual magnetic nanodots.

Fig. 1. Schematic diagram of Room Temperature Scanning Hall Probe Microscope (RT-SHPM), a 50nm Bismuth Hall sensor, Magnetic &.topographic images of a CoCrTa Hard Disk

SHPMs are becoming indispensable tools for characterizing the magnetic materials at (~50nm) scale quantitatively and non-invasively. Improvements in the spatial resolution (~20-30nm), time resolution (~ps) and scan speed (~8-10 Frames/s) are all feasible, opening up new possibilities, which can not be imagined before.

#### References

A. Oral, S. J. Bending and M. Henini, Appl. Phys. Lett., 69, 1324 (1996).

A. Sandhu, K. Kurosawa , M. Dede, A. Oral, Jpn. J. Appl. Phys. 43, 777 (2004)

A. J. Brook, S. J. Bending, J. Pinto, A. Oral, D. Ritchie, H. Beere, M. Henini, and  A.Springthorpe, Appl. Phys. Lett. 82, 3538 (2003)

Low Temperature Scanning Hall Probe Microscope (LT-SHPM) and Room Temperature Scanning Hall Probe Microscope (RT-SHPM), NanoMagnetics Instruments Ltd. Suite 290, 266 Banbury Road, Oxford, U.K. www.nanomagnetics-inst.com